Reg. No. ________

Karunya University

(Declared as Deemed to be University under Sec.3 of the UGC Act, 1956)

End Semester Examination – November / December 2008

Subject Title: 	MATERIAL SCIENCE								              Time : 3 hours

Subject Code: 	EE223			         						                Maximum Marks: 100

#### Answer ALL questions

PART – A  (10 x 1 = 10 MARKS)

1.	Define Fermi level.

2.	Write down Fermi-Dirac distribution function.

3.	When does an intrinsic semiconductor behave like an insulator?

4.	_________are the majority charge carriers in p-type semiconductor.

5.	What is meant by Bloch wall energy in Ferromagnetism?

6.	Define dielectric loss.

7.	Write the name of the any one LCD materials.

8.	What do you mean by an exciton?

9.	List any two bone biomaterials.

10.	What are non-linear materials?

PART – B  (5 x 3 = 15 MARKS)

11.	Explain the following: (a) Meissner effect 	(b) Isotope effect in superconductors.

12.	List out the important outcomes of Hall effect experiment.

13.	What is meant by magnetic susceptibility? Derive the relation between magnetic       susceptibility () and permeability (r).

14.	Explain thermography with a block diagram.

15.	Write a note on ceramic magnets.

PART – C  (5 x 15 = 75 MARKS)

16.	Deduce the mathematical expression for electrical conductivity and thermal conductivity of a conducting material and hence obtain Wiedemann-Franz law.

(OR)

17.	a.	Derive the equation of density of states in a conducting material and list out

its importance.																(12)

b.	What are the applications of high resistivity materials? Give examples.					(3)

18.	Obtain the expression for density of charge carriers in an intrinsic semiconductor. Show the variation of Fermi level with temperature.

(OR)

19.	a.	What is Hall Co-efficient? Show that for a p-type semiconductor the Hall coefficient RH is

inversely proportional to the number of hole.										(10)

b.	Describe an experimental setup for the measurement of Hall voltage.				(5)

20.	a.	Explain the reason for the formation of domain structure in ferromagnetic material and how

the hysteresis curve is explained on the basis of the domain theory.					(9)

b.	Explain the following:  (a) magnetic bubble memory		(b) magnetic shift register	(3+3)

(OR)

[P.T.O]

21.	a.	Derive the Clausius-Mosotti equation and explain its use in predicting the dielectric constant

of solids.																	(10)

b.	Discuss in detail the various dielectric break down mechanism.					(5)

22.	a.	Explain the optical properties of metals, Insulators and semiconductors.

b.	Explain the construction and working of seven segment LED display.

(OR)

23.	a.	Give the construction and working of field effect or twisted neumatic LCD.

b.	Explain with block diagram the application of thermography in medical field.

24.	a.	What are metallic glasses? How are they prepared? Explain its use as transformer core

material.

b.	Discuss different possible structure of polymers.

(OR)

25.	a.	Explain the origin of nonlinear optics. How are Second Harmonic Waves generated? Give

example for organic NLO materials.

b.	Write an essay on biomaterials and its modern applications in the filed of medicine.