Reg. No. ________

Karunya University

(Karunya Institute of Technology and Sciences)

(Declared as Deemed to be University under Sec.3 of the UGC Act, 1956)

End Semester Examination – April/May – 2016

Subject Title :	METAL CUTTING THEORY AND PRACTICE		      	     Time : 3 hours

Subject Code:	09ME223								 		       Maximum Marks: 100

#### Answer ALL questions

PART – A  (10 x 1 = 10 MARKS)

1. 	Define continuous chip with built up edge.

2. 	State the importance of the cutting ratio.

3. 	Is the relief angle important?

4. 	List the requirement of a dynamometer for measuring forces in cutting.

5. 	Why are tool temperatures low at low cutting speeds and high at high cutting speeds?

6. 	What is hot machining?

7. 	Give reason that pure aluminum and copper are generally rated as easy to machine.

8. 	State the application of Taylor’s tool life equation.

9. 	What is chatter in machining?

10. 	List the parameter affecting grinding process.

PART – B  (5 x 3 = 15 MARKS)

11. 	State the function of chip breakers and how do they work?

12. 	Sketch the forces during turning.

13. 	List some of the important properties of cutting fluids.

14. 	Explain the reasons that the same tool life may be obtained at two different cutting speeds.

15.	Mention the various types of chatters in machining.

PART – C  (5 x 15 = 75 MARKS)

16. 	A 50 mm outside diameter mild steel tubing is turned on a lathe with cutting speed of 20 m/min with a tool having rake angle of 35°. The tool is given a feed of 0.1 mm/rev and it is found by dynamometer that the cutting forces is 2500 N and feed force is 1000 N. Length of the continuous chip in one revolution is 80 mm. Calculate the coefficient of friction, shear plane angle, velocity of chip along tool face and chip thickness.

(OR)

17. 	Show schematically the Merchant’s force circle in orthogonal cutting. Derive the equations for shear and friction forces in terms of the material properties and cutting process parameters.

18. 	a. 	Discuss the tool nomenclature and the effect of different tool angles on machinability and 	the tool performance in any machining operation.								            (8)

b. 	Discuss the various parameters and their significance, taking single point cutting tool as an  example.  													        			    (7)

(OR)

19. 	a. 	Discuss the force system which comes to picture during milling operation.	          	    (8)

b. 	Explain the effect of helix angle on force system in milling.                                      	    (7)

20. 	Explain any two methods that can be used for heat and temperature determination during metal cutting.

(OR)

[P.T.O.]

21. 	a. 	Explain the action of cutting fluids in detail. 										    (7)         b.	Enumerate the types of cutting fluids and mention the composition and applications of any 	three types.        												        			    (8)

22. 	a. 	Write a short note on ISO specifications for inserts and tool holders. 			           (7)

b. 	What is optimum tool life? How is it determined? 								    (8)

(OR)

23. 	Explain the following

a. 	Tool life testing. 										        					    (8)

b. 	Economics of metal machining and its importance. 						        	    (7)

24. 	Write notes on the following

a. 	Measurement of wear of cutting tools in machining.					                    	    (8)

b. 	Crater wear. 										                    					    (7)

(OR)

25. 	Discuss the mechanism of grinding in detail. Also describe the cutting action of the grit and effect of grid force on wheel wear.