Reg. No. ________

Karunya University

(Karunya Institute of Technology and Sciences)

(Declared as Deemed to be University under Sec.3 of the UGC Act, 1956)

End Semester Examination – April/May – 2016

Subject Title :	FATIGUE AND FRACTURE MECHANICS			      	     Time : 3 hours

Subject Code:	12AE225								 		       Maximum Marks: 100

#### Answer ALL questions

PART – A  (10 x 1 = 10 MARKS)

1.	Define fatigue notch factor.

2.	Define notch sensitivity index.

3.	What is Neuber’s rule?

4.	What is the need for cycle counting technique?

5.	Define dislocations of materials.

6.	What are the applications of strain-life approach?

7.	What are the advantages of stress - life approach?

8.	Define energy release rate (G) in crack growth.

9.	Define safe life design.

10.	What are the factors affecting fatigue?

PART – B  (5 x 3 = 15 MARKS)

11.	Explain the methods of reducing stress concentrations.

12.	Write the Soderberg, Modified Goodman and Gerber relations.

13.	What is SN curve? Explain the significant points in the curve.

14.	What are the three modes of loading in fracture mechanics? Explain with neat sketches.

15.	Write the procedures followed while designing against fatigue?

PART – C  (5 x 15 = 75 MARKS)

16.	a.	The fatigue (endurance) limit of a 1045 (plain carbon) steel is about 300 MN/m2 when the 	mean stress is zero. The tensile strength of this steel is 750 MN/m2. Using Goodman 	equation, estimate the safe stress amplitude for 1045 steel for the situation mean stress of 	250 MN/m2. 																	    (5)

b.	Derive the expression of shear stress and shear strain for ductile single crystals.		  (10)

(OR)

17.	a.	A circumferentially notched cylindrical rod of a high-strength, low alloy steel is subjected 	to repeated bending at a nominal stress amplitude, Sa = 250 MPa, and a mean stress, 	Sm=275 MPa. For the notch geometry of the rod, the elastic stress concentration factor,

Kt, and the notch sensitivity index, q are 2.3 and 0.15 respectively. Fully reversed cyclic stress tests conducted on smooth laboratory specimens give following material parameter for the Basquin equation.σf' = 1000 MPa and b = -0.12. The endurance limit was estimated from the tests to be 280 MPa. The yield and tensile strengths of the steel are σy= 700 MPa and σTS= 1050 Mpa. Estimate the high-cycle fatigue life of notched rod.

(7)

b.	Draw typical S-N curves for mild steel and aluminum and explain the differences.	    (4)

c.	Shortly explain Total- life approach and Defect-tolerant approach.					    (4)

[P.T.O]

18.	Explain Cycle counting techniques.

(OR)

19.	a.	Explain Coffin Mansion’s relation of fatigue behavior.							    (5)

b.	Discuss the miner’s cumulative damage theory.									    (5)

c.	Shortly explain low and high cycle fatigue with sketch.							    (5)

20.	Explain the types of dislocation of the materials.

(OR)

21.	Explain the mechanism of fatigue crack growth. What are the various factors that influence the fatigue crack growth? With neat sketches, explain different modes of crack growth.

22.	Explain Griffith’s theory and compare this theory to Irwin- Orwin extension.

(OR)

23.	a.	Explain the effect of thickness on fatigue toughness.								    (7)

b.	Explain the stress intensity factor for typical crack geometries.  					    (8)

24.	a.	Explain: ‘Designing against fatigue in aircraft’.									    (8)

b.	Discuss a few fatigue problems encountered in subsonic and supersonic aircraft.		    (7)

(OR)

25.	a.	Explain the safe life and fail safe design philosophies.						    		    (8)

b.	Explain the fatigue failure of comet airplane cabin structure failure. 				    (7)