.Reg. No. ________

Karunya University

(Karunya Institute of Technology and Sciences)

(Declared as Deemed to be University under Sec.3 of the UGC Act, 1956)

End Semester Examination – April/May-2013

Subject Title: ENGINEERING MATERIALS AND APPLICATIONS	       	       Time: 3 hours

Subject Code: 12ME306						         			      	       Maximum Marks: 100

Answer ALL questions (5 x 20 = 100 Marks)

1.	Compulsory:

a.	What is meant by basic composites? Why fillers are added to composites?   	 		(4)

b.	Give a detailed account of different fiber materials by giving their properties, applications, 	advantages and limitations.													(6)

c.	List the different methods available for processing of polymer matrix composites. Explain 	in detail any two methods. 													(6)

d.	A unidirectional composite is composed of 65% volume of carbon fibers (modulus 240 GPa) in a epoxy resin matrix (Modulus 4 GPa). Calculate the longitudinal modulus of the composite. 			 				            									(4)

2.	a.	What is meant by dislocation? Explain the two types of dislocation with neat sketches. 			Outline the three stages in the movement of an edge dislocation.					(10)

b.	Explain the terms slip, slip line and slip plane with a schematic drawing. Derive an  				expression for critical resolved shear stress for slip. Why critical shear stress is higher for 			Titanium and lower for silver.													(10)

(OR)

3.	a.	Explain the following based on working hardening:   								(10)

i.	Generalised flow curve for FCC single crystals and three stages of a flow curve.

ii.	Effect of specimen orientation on the shape of a flow curve.

iii.	Variation of tensile properties with amount of cold work.

iv.	Recovery, recrystallization and grain growth.

b.	What is Twinning? Explain the difference between slip and Twinning. Describe twinning 	with a classical picture. 														(10)

4.	a.	Describe the mechanism of crack propagation for both ductile and brittle modes of 				fracture.  																	(10)

b.	Explain three stages of a creep curve; give a detailed account of creep resistant materials 			and mechanisms of creep deformation.                                               				(10)

(OR)

5. 	a.	What is the purpose fatigue tests? Explain rotating beam fatigue testing machine with a 	neat sketch. Give a detailed account of mechanisms of fatigue failure.				(10)

b.	i.	Explain Grifths theory of fracture.											(5)

ii.	Explain in detail different factors affecting fatigue life.						(5)

6. 	a.	Explain in detail precipitation hardening of Aluminium – Copper alloy.      	 		(10)

b.  	What is TRIP steel? What are the advantages of TRIP steels? Give the typical composition   		and processing sequence for TRIP steel. 										(10)

(OR)

7.	a.	Why a steel is called a Maraging steel? Give the typical composition and properties of 	maraging steel. Explain detail the manufacturing sequence of maraging steel. 		(10)

[P.T.O]

b.	Explain in brief the following: 													(10)

i.	Patenting of steel wire.

ii.	Micro alloyed steels.

iii.	Shape memory alloys.

iv.	Metallic glasses.

8. 	a.	Explain in detail classification of ceramics based on applications and give one application 	for each type of ceramics. 														(10)

b.	Give a detailed account of glasses by giving their composition, properties, manufacture 			and applications.																(10)

(OR)

9. 	a.	What are different types of refractories? Give the important properties of refractories and 	explain the various steps in the manufacture of silica refractories. 					(10)

b. 	Explain in detail the following processes: 										(10)

i.	Annealing of glass.

ii.	Glass Tempering.

iii.	Heat Treatment of glass ceramics.