Reg. No. ________

Karunya University

(Karunya Institute of Technology and Sciences)

(Declared as Deemed to be University under Sec.3 of the UGC Act, 1956)

End Semester Examination – April/May-2013

Subject Title: MATERIAL SCIENCE AND ENGINEERING		       		       Time: 3 hours

Subject Code: ME283				       						              Maximum Marks: 100

#### Answer ALL questions

PART – A (10 x 1 = 10 MARKS)

1.	Define Miller Indices

2.	List some examples of FCC crystal structure materials.

3.	What is meant by slip in plastic deformation?

4.	Define point defects in lattice structure.

5.	Write the mechanisms of creep.

6.	State Griffith’s theory of crack propagation.

7.	What is meant by phase diagram?

8.	How are solid solutions classified?

9.	What are the objectives of normalizing?

10.	List the different surface hardening processes used in steel.

PART – B (5 x 3 = 15 MARKS)

11.	Calculate the density of copper which has an atomic radius of 0.128nm, an FCC crystal structure and atomic weight of 63.5g/mol.

12.	What is the effect of diffusion species on diffusion mechanism?

13.	Distinguish between ‘ductile’ and ‘brittle’ fractures.

14.	Describe the general applications of phase rule.

15.	What are the objectives of annealing?

PART – C (5 x 15 = 75 MARKS)

16.	a.	Sketch the unit cells of the F.C.C and H.C.P structures.							(5)		b. 	Draw the following planes and directions in a F.C.C structure. (001): (111); [110], [101] 																						(10)

(OR)

17.	Briefly explain the various steps of specimen preparation in metallographic analysis.

18.	Distinguish between slip and twinning as modes of plastic deformation of metal and alloys.

(OR)

19.	Explain the following terms:

a. 	Recovery.
       	b. 	Recrystallization.
       c.	Grain growth	.

20.	What is creep of metals? Draw a typical creep curve and explain the three stages of creep.

(OR)

21.	Describe with the aid of sketches the apparatus, specimen and procedure to be followed for fatigue test. Explain briefly prevention of fatigue failure.

22.	Explain the Hume Rothery rules as applied to the formation of solid solution.

(OR)

[P.T.O]

23.	a.	What is the difference between an Iron carbon diagram and a T-T-T diagram? 		(5)		b. 	Under what conditions do the pearlite and bainite transformations take place? 		(10)

24.	Name the different annealing processes. Is spheroidising different from annealing? Explain.

(OR)

25.	Discuss nitriding as a method of surface hardening of steel and compare it with induction-hardening.