Reg.No. ____________

End Semester Examination – Apr/May – 2018

| # Code : | # 16NT3004 | # Duration : | # 3hrs |
| --- | --- | --- | --- |
| # Sub. Name : | # MAGNETIC NANOMATERIALS AND NANOFLUIDS | # Max. marks : | # 100 |

ANSWER ALL QUESTIONS (5 × 20 = 100 Marks)

| Q. No. | Sub Div. | Questions | Course Outcome | Marks |
| --- | --- | --- | --- | --- |
| 1. | a. | Derive the ground state multiplicities and the value of Russel–Saunders coupling of Eu3+ and Tb3+ | CO1 | 4 |
|  | b. | Match the following: Magnetic induction; Am2 kg-1. Mass magnetization; Tesla. Magnetic moment; m3 kg. Mass susceptibility; Am2. | CO2 | 4 |
|  | c. | Identify from the magnetization plot which kind of magnetic material this magnetic behavior corresponds to: Justify your answer in one or two sentences. | CO1 | 4 |
|  | d. | Define: Morin transition, Curie temperature. | CO1 | 4 |
|  | e. | The magnetic field strength in silicon is 1000 A/m. If the magnetic susceptibility is −0.25 × 10−5, calculate the magnetization and flux density in silicon. Interpret from your answer, silicon is which kind of magnetic material. | CO4 | 4 |
| (OR) |  |  |  |  |
| 2. | a. | Match the following magnetization curves with the ferrite materials of same size mentioned in the second column. - CaFe2O4 NPs - CaFe2O4 NPs coated with PEG polymer. - 5% Mn doped ZnO - As prepared ZnO. - MnFe2O4 NPs - ZnFe2O4 NPs. - Fe3O4 NPs - Fe3O4 NPs coated with PVA polymer. | CO2 | 4 |
|  | b. | Explain the phenomenon of ferrimagnetism with the key points on its origin. | CO2 | 4 |
|  | c. | What are meant by gyromangnetic ratio and Landé’s ‘g’ factor? | CO1 | 4 |
|  | d. | Replace the question marks in the following hysteresis loop with suitable magnetic parameters. | CO2 | 4 |
|  | e. | A paramagnetic material has FCC structure with a cubic edge of 2.5 A°. If the saturation value of magnetization is 1.8 × 106 A m–1, Calculate the magnetization contributed per atom in Bohr magnetrons. | CO1 | 4 |
| 3. | a. | In the following figures, identify the magnetic hard and easy axes of the crystal. Mark each of the magnetization curves with the corresponding magnetic axes. | CO2 | 4 |
|  | b. | Explain thermal and alternating field demagnetization techniques. | CO1 | 4 |
|  | c. | If the frequency factor of a sample of superparamagnetic nanoparticles of size 10 nm is 2 × 10-9 s-1 and its relaxation time is 20 nanoseconds, calculate the anisotropy constant value of the magnetic naoparticles at 25 °C. | CO4 | 4 |
|  | d. | Mention the types of remanence. Write the reason for the origin of each type. | CO3 | 4 |
|  | e. | Define: magnetostatic energy and magnetostriction. | CO1 | 4 |
| (OR) |  |  |  |  |
| 4. | a. | The following are the temperature-dependent magnetization profiles of CoFe2O4 nanoparticles of various sizes. Match the schematically represented nanoparticles with their magnetization profiles. | CO3 | 4 |
|  | b. | Describe shape anisotropy and its contribution to magnetism of materials. | CO2 | 4 |
|  | c. | Briefly explain the single domain nanoparticles. | CO2 | 4 |
|  | d. | Observe the following images of iron oxide nanoparticles. Assuming that the width of the nanoparticles is the same in all the three cases, which of these samples will have more anisotropic contribution to magnetism? Justify your answer. |  | 4 |
|  | e. | Match the following: Fe2+; 4f3. Ni2+; 4f5. Zn2+; 4f10. Nd3+; 4f13. Sm3+; 3d6. Ho3+; 3d10. Er3+; 3d8. Yb3+; 4f11. | CO4 | 4 |
| 5. | a. | The following table lists out the magnetic moments of iron group ions. There are large differences between the experimental and the calculated values of the moments of each of the ions. Account for this general difference. Ion; Magnetic moment in Bohr magnetron. Experimental; Calculated. Fe2+; 5.4; 6.7. Co2+; 4.8; 6.6. Ni2+; 3.2; 5.6. Mn2+; 5.9; 5.5. Mn3+; 4.9; 0. | CO3 | 4 |
|  | b. | Write the Hamiltonian representing the paramagnetic susceptibility of lanthanide ions under the Coulomb potential of the nucleus and having the contributions from inter-electron repulsion and spin-orbit coupling. Explain the various terms involved in the Hamiltonian. | CO3 | 4 |
|  | c. | Compared to the electronic moment, the nuclear magnetic moment does not significantly contribute to the net magnetic moment of a magnetic material. Justify the statement. | CO3 | 4 |
|  | d. | Highlight the concept of quenching of orbital angular momentum by the crystal field of ligands. | CO2 | 4 |
|  | e. | Briefly explain the principle of a superconducting quantum interference device. | CO2 | 4 |
| (OR) |  |  |  |  |
| 6. | a. | Illustrate using the case of hydrogen molecule the total electronic wave function has a contribution from exchange integral. Explain the significance of the sign of the exchange integral on magnetism. | CO3 | 12 |
|  | b. | Describe the concept of super-exchange interaction in transition metal oxides. | CO3 | 4 |
|  | c. | Explain specific heat anomaly in magnetic materials. | CO3 | 4 |
| 7. | a. | The ground state configuration of magnetic materials in their reduced dimensions is influenced by Kondo and RKKY screening. Justify the statement. | CO1 | 4 |
|  | b. | Explain the influence of geometrical arrangement and surface symmetry on the magnetism of materials of reduced dimensions. | CO1 | 8 |
|  | c. | Write notes on the magnetism of free nanoparticles and nanoparticles in contact with surfaces. | CO5 | 8 |
| (OR) |  |  |  |  |
| 8. | a. | Arrange the following permanent magnets in the order of their possible magnitude of coercivity: AlNiCo 5, Nd2Fe14B (sintered), SrFe2O4, Nd2Fe14B (bonded). | CO5 | 4 |
|  | b. | Indicate the magnetic nature of the elements as dia-, para-, ferro-, and anti-ferromagnetic and convert this periodic table into a magnetic periodic table: | CO1 | 4 |
|  | c. | Choose the best answer: The theorem of Bohr and von Leeuwen explained the ……… - Vanishing of average magnetization classically - Enhancement of orbital angular momentum - Bohr magneton - Electronic spin states | CO3 | 1 |
|  | d. | Choose the best answer: The value of gJ is experimentally determined by ……… - Measuring the spin angular momentum - Measuring the magnetization in an applied magnetic field - Measuring the Curie temperature - Measuring the diamagnetic susceptibility | CO4 | 1 |
|  | e. | Choose the best answer: C/T is ……. - Magnetic susceptibility - Magnetization - Inverse of magnetization - Inverse of magnetic susceptibility | CO2 | 1 |
|  | f. | Choose the best answer: The molecular field concept was hypothesized by ……… - Schrödinger - Uhlenbeck - Weiss - Von Leeuwen | CO4 | 1 |
|  | g. | Choose the best answer: The state represented by is ……… - Symmetric singlet state - Anti-symmetric singlet state - Symmetric triplet state - Anti-symmetric triplet state | CO4 | 1 |
|  | h. | Choose the best answer: The following temperature dependence of magnetic susceptibility corresponds to ………. material. - Diamagnetic - Paramagnetic - Ferromagnetic - Antiferromagnetic | CO1 | 1 |
|  | i. | Explain the relationship between superparamagnetism and blocking temperature. | CO4 | 6 |
|  |  | Compulsory: |  |  |
| 9. | a. | Discuss any one method of preparation of calcium ferrite nanoparticles. | CO1 | 5 |
|  | b. | Match the following: Kupfer cells; 7 nm magnetic nanoparticles. Macrophage uptake; 250 nm nanoparticles. Glomerular endothelium; Bare magnetic nanoparticles. Serum proteins; Coating with CD47 peptides. Escaping phagocytic clearance; Opsonization of magnetic nanoparticles. | CO5 | 5 |
|  | c. | There are three samples of magnetic materials viz., sphere-shaped nanoparticles of size 8 nm, rod-shaped nanoparticles of diameter 180 nm, and disc-shaped nanoparticles of size 75 nm. Which sample is the best suited for magnetic-field assisted drug delivery? Justify your answer with suitable reasons. | CO5 | 5 |
|  | d. | Explain the hyperthermia application of magnetic nanomaterials. | CO5 | 5 |