Reg.No. ____________

End Semester Examinations – Nov/Dec – 2018

| Code : | 17ME3009 | Duration : | 3hrs |
| --- | --- | --- | --- |
| Sub. Name : | ENGINEERING FRACTURE MECHANICS | Max. marks : | 100 |

ANSWER ALL QUESTIONS (5 x 20 = 100 Marks)

| Q. No. | Sub Div. | Questions | Course Outcome | Marks |
| --- | --- | --- | --- | --- |
| 1 | a. | Discuss the Griffith failure and analysis for safe crack using strain energy release rate. | CO1 | 12 |
|  | b. | Differentiate intergranular and transgranular fracture and state why swords offer more resistance to fracture. | CO3 | 8 |
| (OR) |  |  |  |  |
| 2. | a. | What are the modes of fracture? Explain its mechanisms. | CO3 | 12 |
|  | b. | Discuss the characteristics of ductile fracture and brittle fracture. | CO3 | 8 |
| 3. |  | Derive the correction of plastic zone size to accommodate stresses in yield zone using Irwin and Dugdale-Barenblatt approach | CO2 | 20 |
| (OR) |  |  |  |  |
| 4. | a. | What is safe crack? What is the role of safe crack in stability and unstability of fracture? | CO3 | 13 |
|  | b. | The fracture resistance is decreasing when the material is subjected to lower temperature. State the reason. | CO2 | 7 |
| 5. | a. | Why R curve is a straight line for brittle material? How it is varied for ductile material? | CO3 | 14 |
|  | b. | Explain, why the crack tip plays vital role in fracture mechanics? | CO1 | 6 |
| (OR) |  |  |  |  |
| 6. |  | Explain J integral and drive the expression of J integral for beam with usefulness. | CO6 | 20 |
| 7. | a. | An bar of steel alloy used to conduct a J integral test. The specimen had dimensions of B = 10 mm, W = 20 mm, S = 80 mm and a = 10 mm. The alloy possessed the following mechanical properties: E = 20 GPa and μ = 0.25. The area of the curve = 5 m2 and the maximum load = 15 kN. Calculate the value of J for this material. | CO6 | 12 |
|  | b | Discuss briefly S N fatigue curve. | CO5 | 8 |
| (OR) |  |  |  |  |
| 8. |  | Derive the crack instability in residual stress fields and explain in detail. | CO3 | 20 |
|  |  | Compulsory: |  |  |
| 9. |  | List the different types defects that can be identified using non destructive techniques. Discuss the common non destructive techniques used for defect detecting. | CO4 | 20 |