Reg.No. ____________

End Semester Examination – Nov/Dec – 2017

| Code : | 17EC3034 | Duration : | 3hrs |
| --- | --- | --- | --- |
| Sub. Name : | VLSI TECHNOLOGY | Max. marks : | 100 |

ANSWER ALL QUESTIONS (5 x 20 = 100 Marks)

| Q. No. | Sub Div. | Questions | Course Outcome | Marks |
| --- | --- | --- | --- | --- |
| 1. | a. | Enumerate the steps to be followed in silicon shaping. | CO1 | 10 |
|  | b. | Reproduce the processing considerations in crystal growth and wafer preparation. | CO1 | 10 |
| (OR) |  |  |  |  |
| 2. |  | Paraphrase in detail about the Molecular Beam Epitaxy. | CO2 | 20 |
| 3. |  | Ponder over the oxide properties in terms of masking properties and oxide charges. | CO1 | 20 |
| (OR) |  |  |  |  |
| 4. | a. | Associate the thermal oxidation process of polycrystalline silicon that is employed in interlevel dielectric for multilayer structures. | CO4 | 10 |
|  | b. | Examine the oxide stress associated with a film. | CO4 | 10 |
| 5. | a. | Tabulate the different types of lithography available in semiconductor IC fabrication. | CO2 | 5 |
|  | b. | Enumerate and extend in detail about the various steps involved in lithography that adopts UV rays. | CO2 | 15 |
| (OR) |  |  |  |  |
| 6. | a. | State the back scattering effect in electron beam lithography. | CO2 | 4 |
|  | b. | Extend the lithography method adopted to overcome the back scattering effect that happens in e-beam lithography. | CO2 | 16 |
| 7. | a. | Analyze in detail about the various effect in the diffusivities of Boron, Phosphorus, Arsenic and Antimony. | CO5 | 10 |
|  | b. | Examine about the diffusion in Polysilicon. | CO5 | 10 |
| (OR) |  |  |  |  |
| 8. | a. | Compare the diffusion enhancement and retardation for various elements and for various treatments. | CO2 | 8 |
|  | b. | With a schematic diagram of ion-implantation, explain its operation and the quantities that define an ion implantation step. | CO2 | 12 |
|  |  | Compulsory: |  |  |
| 9. | a. | Summarize the NMOS IC technology. | CO6 | 10 |
|  | b. | Reproduce the CMOS IC technology. | CO6 | 10 |

ALL THE BEST